Space product assurance

ECSS Secretariat

ESA-ESTEC

Requirements & Standards Division

Noordwijk, The Netherlands

Requirements for manufacturing and procurement of threaded fasteners

Foreword

This Standard is one of the series of ECSS Standards intended to be applied together for the management, engineering and product assurance in space projects and applications. ECSS is a cooperative effort of the European Space Agency, national space agencies and European industry associations for the purpose of developing and maintaining common standards. Requirements in this Standard are defined in terms of what shall be accomplished, rather than in terms of how to organize and perform the necessary work. This allows existing organizational structures and methods to be applied where they are effective, and for the structures and methods to evolve as necessary without rewriting the standards.

This Standard has been prepared by the ECSS Executive Secretariat, endorsed by the Document and Discipline Focal points, and approved by the ECSS Technical Authority.

Disclaimer

ECSS does not provide any warranty whatsoever, whether expressed, implied, or statutory, including, but not limited to, any warranty of merchantability or fitness for a particular purpose or any warranty that the contents of the item are error-free. In no respect shall ECSS incur any liability for any damages, including, but not limited to, direct, indirect, special, or consequential damages arising out of, resulting from, or in any way connected to the use of this Standard, whether or not based upon warranty, business agreement, tort, or otherwise; whether or not injury was sustained by persons or property or otherwise; and whether or not loss was sustained from, or arose out of, the results of, the item, or any services that may be provided by ECSS.

Published by: 	ESA Requirements and Standards Division

ESTEC, P.O. Box 299,

2200 AG Noordwijk

The Netherlands

Copyright: 	2008 © by the European Space Agency for the members of ECSS

Change log

| ECSS-Q-70-46A 21 January 2000 | First issue Transforming ESA PSS-01-746 into an ECSS Standard |
| --- | --- |
| ECSS-Q-ST-70-46C 31 July 2008 | Second issue Redrafting of ECSS-Q-70-22A according to new ECSS drafting rules and template. In particular: - The requirements of the original clauses 4, 5, 6 and 7 were moved to the clauses 4.1 to 4.4. - From the sections 4.3.7and 4.3.8 the requirements which do not fit there were moved to section 4.1.2 as requirements g and h. - From the original section 7.2.5 a DRD was created and moved to the normative Annex B. - Table C- was moved to the informative Annex C. - The section 4 “Principles” was deleted.. |
| ECSS-Q-ST-70-46C Rev.1 6 March 2009 | Second issue revision1 Changes with respect to version C (31 July 2008) are identified with revision tracking. Main change concern the addition of a normative reference (DIN ISO 9152) and the addition of a new requirement (4.2.5.h) calling this reference. |

Table of contents

Change log	3

1 Scope	6

2 Normative references	7

3 Terms, definitions and abbreviated terms	9

3.1	Terms defined in other standards	9

3.2	Terms specific to the present standard	9

3.3	Abbreviated terms	10

4 Requirements	11

4.1	Fabrication	11

4.1.1	General	11

4.1.2	Raw material	11

4.1.3	Head forming	11

4.1.4	Heat treatment	12

4.1.5	Headtoshank fillet rolling	12

4.1.6	Threads	12

4.1.7	Identification marking	13

4.1.8	Surface treatment	13

4.1.9	Workmanship, handling and packaging	13

4.2	Dimensional and metallurgical requirements	14

4.2.1	General	14

4.2.2	Nominal dimensions	14

4.2.3	Headtoshank fillet	14

4.2.4	Nondestructive inspections	15

4.2.5	Metallurgical examination	16

4.2.6	Measurement of hydrogen content	17

4.2.7	Outgassing and offgassing	17

4.3	Mechanical testing	18

4.3.1	General	18

4.3.2	Hardness test	18

4.3.3	Tensile test	19

4.3.4	Shear test	20

4.3.5	Fatigue test	21

4.3.6	Creep test	21

4.3.7	Corrosion test	23

4.3.8	Stresscorrosion test	23

4.4	Quality assurance	24

4.4.1	General	24

4.4.2	Quality requirements	24

Annex A (normative) Customer specification document for threaded fasteners – DRD	27

Annex B (normative) Product conformance report (PCR) – DRD	29

Annex C (informative) Inspection levels, acceptance quality limits (AQL) and limiting quality levels (LQ) for inspection of fasteners	31

Figures

Figure 4-1: Tolerance of headtoshank fillet profile	15

Figure 4-2: Location of microsections for metallurgical examination	16

Figure 4-3: Area delimiting interruptions in grain flow in the headtoshank region	17

Figure 4-4: Example of a regular grain flow in a threaded surface	17

Figure 4-5: Locations for hardness testing (indicated with cross symbol)	19

Figure 4-6: Loading schematic for tensile testing of threaded fasteners	22

Figure 4-7: Schematic of an example of doubleshear loading jigs	23

Tables

Table 4-1: Maximum allowed values of the extension C of the distorted area shown in Figure 4-1	15

Table C- 1: Inspection levels, acceptance quality limits (AQL) and limiting quality levels (LQ) for inspection of fasteners	31

# Scope

This Standard defines the requirements for manufacturing, provision, inspection and quality control of highquality threaded fastening devices (bolts, nuts, studs and screws) hereafter referred to as threaded fasteners or fasteners, used in space hardware.

This Standard does not include a complete review of the factors relevant to the fabrication of high quality threaded fasteners. It provides the definition of the technical requirements and quality control procedures to be applied in the fabrication and supply of threaded fasteners for spacecraft applications.

Fasteners for spacecraft applications are those aerospace standard fasteners (i.e. in accordance with LN, DIN or other national or international aerospace standards), or those fasteners meeting or exceeding the requirements in ISO 4759-1 for “Product grade A”, which also fulfil the requirements for space applications as specified in the present document.

# Normative references

The following dated normative documents are called by the requirements of this ECSS Standard and therefore constitute requirements to it. Subsequent amendments to, or revisions of any of these publications do not apply.

- However, parties to agreements based on this ECSS Standard are encouraged to investigate the possibility of applying the most recent editions of the normative documents indicated below.

| ECSS-S-ST-00-01C | ECSS system – Glossary of terms |
| --- | --- |
| ECSS-E-ST-30-01C | Space engineering — Fracture control |
| ECSS-Q-ST-70C | Space product assurance — Materials, parts and processes |
| ECSS-Q-ST-70-02C | Space product assurance — Thermal vacuum outgassing test for the screening of space materials |
| ECSS-Q-ST-70-29C | Space product assurance — The determination of offgassing products from materials and assembled articles to be used in a manned space vehicle crew compartment |
| ECSS-Q-ST-70-36C | Space product assurance — Material selection for controlling stresscorrosion cracking |
| ECSS-Q-ST-70-37C | Space product assurance — Determination of the susceptibility of metals to stress— corrosion cracking |
| ECSS-Q-ST-70-71C | Space product assurance — Data for selection of space materials |
| ISO 204 | Metallic materials — Uninterrupted uniaxial creep testing in tension — Method of test |
| ISO 225 | Fasteners — Bolts, screws, studs and nuts — Symbols and designations of dimensions |
| ISO 1502 | ISO general — purpose metric screw threads — Gauges and gauging |
| ISO 2859-1 | Sampling procedures for inspection by attributes, Part 1: Sampling schemes indexed by acceptance quality limit (AQL) for lotbylot inspection |
| ISO 2859-2 | Sampling procedures for inspection by attributes, Part 2: Sampling plans indexed by limiting quality (LQ), for isolated lots inspection |
| ISO 3353-1:2002 | Aerospace — Lead and runout threads — Part 1: Rolled external threads |
| ISO 3800 | Threaded fasteners – Axial load fatigue testing – Test methods and evaluation of results |
| ISO 4759-1 | Tolerances for fasteners — Part 1: Bolts, screws, studs and nuts — Product grades A, B and C |
| ISO 6157-2 | Fasteners — Surface discontinuities – Part 2: Nuts |
| ISO 6157-3 | Fasteners – Surface discontinuities – Part 3: Bolts, screws and studs for special requirements |
| ISO 6506-1 | Metallic materials — Brinell hardness test — Part 1: Test method |
| ISO 6506-2 | Metallic materials — Brinell hardness test — Part 2: Verification and calibration of testing machines |
| ISO 6506-3 | Metallic materials — Brinell hardness test — Part 3: Calibration of reference blocks |
| ISO 6507-1 | Metallic materials — Vickers hardness test – Part 1: Test method |
| ISO 6507-2 | Metallic materials — Vickers hardness test — Part 2: Verification and calibration of testing machines |
| ISO 6507-3 | Metallic materials — Vickers hardness test — Part 3: Calibration of reference blocks |
| ISO 6508-1 | Metallic materials — Rockwell hardness test — Part 1: Test method |
| ISO 6508-2 | Metallic materials — Rockwell hardness test — Part 2: Verification and calibration of testing machines |
| ISO 6508-3 | Metallic materials — Rockwell hardness test — Part 3: Calibration of reference blocks |
| ISO 9140 | Aerospace – Nuts, plain or slotted (castellated) – Test methods |
| DIN ISO 9152 | Aerospace – Bolts, with MJ Threads, in Titanium alloys, strength class 1100 MPa – Procurement specification |
| ASTM B 117-07a | Standard practice for operating salt spray (fog) apparatus |
| ASTM E 1417-05e1 | Standard practice for liquid penetrant testing |
| ASTM E 1444-05 | Standard practice for magnetic particle testing |

# Terms, definitions and abbreviated terms

## Terms defined in other standards

For the purpose of this Standard, the terms and definitions from ECSS-S-ST-00-01 and ECSS-Q-ST-70 apply.

## Terms specific to the present standard

- bolt

cylindrical screwed bar provided with a head, generally not threaded along its entire length

- For example: Shank plus threaded portion.

- failsafe

approach in which the structure is designed with sufficient structural redundancy to ensure that the failure of one structural element does not cause general failure of the entire structure

- fastener

device used to hold parts firmly together in an assembly

- galling

condition whereby excessive friction between high spots results in localized welding with subsequent splitting and a further roughening of rubbing surfaces of one or both or two mating parts

- nut

metal collar, screwed internally, to fit a bolt

- Usually hexagonal in shape and operated by a spanner.

- safelife

approach which requires that the largest undetected defect that can exist in the structure does not grow to failure when subjected to loads and environments encountered in service

- sampling plan

combination of sample size to be used with associated batch acceptability criteria

- shank

unthreaded portion of the cylindrical screwed bar of a bolt

- stud

shank, or endless bolt, externally screwed from one end, both ends or along its entire length

- (screw) thread

helical ridge of approximately triangular, square or rounded section, formed on a cylindrical core, the pitch and core diameter being standardised under various systems

- threaded fastener

device composed by a cylindrical screwed bar provided with a head and a metal collar, screwed internally, to fit the cylindrical bar that is used to hold parts firmly together in an assembly

## Abbreviated terms

For the purpose of this Standard, the abbreviated terms from ECSS-S-ST-00-01C and the following apply:

| Abbreviation | Meaning |
| --- | --- |
| AQL | acceptance quality level |
| ASTM | American Society for Testing and Materials |
| HB | Brinell hardness |
| HRC | Rockwell hardness |
| HV | Vickers hardness |
| ISO | International Organization for Standardization |
| LQ | limiting quality |
| PCR | product conformance report |
| PVC | polyvinyl chloride |
| RMC | raw material certificate |
| UTS | ultimate tensile strength |

# Requirements

## Fabrication

### General

          - The customer shall establish a specification document in conformance with the DRD in Annex A.

          - The manufacturer shall have a quality assurance system.

          - The manufacturer shall verify and assure conformance during production to the technical requirements specified in this clause.

### Raw material

          - The raw material for threaded fasteners shall be selected in accordance with the metallic materials requirements as per ECSS-Q-ST-70-71C, if not otherwise specified in the customer specification document for threaded fasteners.

          - Nut material shall be more ductile than bolt material.

- The reason is that during tightening nut threads can deflect to seat on the bolt threads.

          - Materials for threaded fasteners shall be selected in order to avoid galling of the mating surfaces.

- Galling in stainless steel fasteners can be prevented by using two different steels on the mating surfaces and by specific surface treatments.

          - Materials for threaded fasteners shall be corrosion resistant

          - Materials shall possess high resistance to stresscorrosion cracking as specified in ECSS-Q-ST-70-36C.

### Head forming

          - Fastener heads shall be formed by hot or cold forging before heat treating.

- Driving recesses and lightening holes in double hexagon design can be forged or machined.

### Heat treatment

          - Headed forged blanks shall be heat treated and cold worked by rolling or drawing methods in accordance with the customer specification document for threaded fasteners and the specifications in clause 4.2 of this Standard.

          - Forged blanks belonging to the same batch shall be heat treated in one batch.

          - The manufacturer shall retreat a batch which, tested as in 4.3.3, did not meet the mechanical property requirements, no more than twice (three times for Titanium alloys).

          - If a different supplier produces the blanks, inspections and quality control shall be performed as specified in 4.4.2.1 under direct responsibility of the original blanks’ supplier.

- This is done in the case where the manufacturer is unable to carry out the blank fabrication as requested by the customer.

          - Grinding of shank and head bearing surfaces of blanks to obtain roughness values as specified in 4.2.4 shall be carried out after any heat treatment.

### Headtoshank fillet rolling

          - Headtoshank fillet rolling shall be carried out after any heat treatment and machining processes.

          - Cold rolling shall remove from the fillet surface any evidence of previous machining or etching process.

          - Geometrical distortion of the fillet surface shall be within the limits specified in 4.2.3.

- In fasteners having compound radii between head and shank, cold rolling can be extended to the remaining part of the fillet surface.

          - There shall be no machining or etching of the fillet radius after rolling.

### Threads

          - External threads shall be formed by rolling process.

          - Thread rolling shall be carried out on each fastener in one single continuous operation.

          - When thread rolling on each fastener is not performed in one single continuous operation, the threaded fasteners shall be submitted to a fatigue test in accordance with 4.3.5.

          - No evidence of machining shall be observed on the thread surface after rolling.

- This applies for fasteners of large diameter, where threads can be machined oversized and subsequently rolled.

          - Thread rolling shall be carried out after heat treatment and machining of fasteners.

          - Unless otherwise specified in the customer specification document for threaded fasteners, a single righthand thread shall be obtained.

          - The thread runout portion of a bolt or stud shall consist in a progressive and regular junction with the shank avoiding sharp changes in section.

          - Thread lead and runout portions shall conform to the requirements in clause 4 of ISO 3353-1:2002.

### Identification marking

          - Fasteners shall be marked by depressed characters only with character size in accordance with the customer specification document for threaded fasteners and drawings.

          - Characters for marking fasteners shall:

            - be depressed no more than 0,25 mm from the surface;

            - have rounded root form;

            - be impressed on the upper surface of the fastener head.

          - Marks shall univocally identify the fastener batch and manufacturer.

          - Safelife fasteners shall be identification marked separately after nondestructive inspection.

### Surface treatment

          - In surface plated fasteners, surface plating shall be applied to the entire fastener surface including the threaded portion.

- Surface plating can cause tolerance variations.

          - Silver plating shall not be used on titanium alloy fasteners.

- Silver and cadmium plating are not used because they can cause embrittlement of titanium alloys, as per requirement in ECSS-Q-ST-70-71C.

          - Baking shall be carried out after plating.

- The reason is to prevent hydrogen embrittlement since electrolytic plating processes generate hydrogen.

          - The baking temperature shall be selected such that the plating and substrate materials are not deteriorated

### Workmanship, handling and packaging

          - Fasteners shall be free from burrs, tool marks, scale, other surface defects and contaminants.

          - Fasteners shall be handled and packed during storage and transportation in the following way:

            - pack fasteners of the same batch in unit packages;

            - do not apply any protective lubricants or substances on fasteners unless otherwise specified in the customer specification document for threaded fasteners.

- This is to prevent mechanical damage and contamination (e.g. from PVC or fibreboard).

          - Each individual package shall be univocally identified by a durable and legible external marking indicating the product denomination, quantity, batch identification, manufacturer, product conformance report as in 4.4.2.5 and date of packing.

          - Fasteners for safelife applications shall be packed and stored separately.

## Dimensional and metallurgical requirements

### General

          - Dimensional and metallurgical controls shall be carried out in accordance with the sampling procedures and acceptance criteria specified in 4.4.2.1.

          - Designation of dimensions and symbols shall be in accordance with ISO 225.

          - Dimensional control of fasteners (bolts, nuts and studs) shall be carried out at room temperature (22  3) C.

          - Gauges and measuring devices shall be in accordance with ISO 1502.

### Nominal dimensions

          - Nominal dimensions shall be in accordance with the detail drawings of the customer specification document for threaded fasteners.

          - All dimensions shall refer to the final product and include any dimensional modification subsequent to chemically applied or electroplated coating.

          - ISO 1502 standards on thread geometry and dimensions shall apply.

          - Tolerances for fasteners shall be in accordance with national or international aerospace standards (e.g. LN, DIN aerospace standards) or meet or exceed tolerance values specified in ISO 4759-1 for “Product grade A”.

### Headtoshank fillet

          - The value of distortion shall not exceed 0,03 mm above and below the profile lines at points A and B in Figure 4-1.

- In bolts, cold rolling of headtoshank fillets can cause distortion of fillet areas. Figure 4-1 shows the typical distortion of the headtoshank fillet profile.

          - The value of the extension C of the distorted area in Figure 4-1 shall not exceed the values indicated in Table 4-1.

### Nondestructive inspections

          - Fasteners shall be free from surface defects such as flaws and inclusions.

          - Inspections on bolts, studs and screws shall be carried out by using liquid penetrant or magnetic particles in accordance with ASTM E 1417-05e1 and ASTM E 1444-05, respectively.

          - Nondestructive inspections shall be carried out by qualified personnel.

          - Fasteners for safelife applications shall be inspected as follows:

            - using a 100 % batch inspection plan;

            - by Xray, ultrasonic or eddy current inspection methods to obtain 95 % (minimum) confidence level and 90 % (minimum) probability of defect detection.

          - For fasteners for safe-life applications the results of NDI shall be evaluated in accordance with clause 10.3 of ECSS-E-ST-30-01C.

          - Fasteners with detected surface defects shall be visually reexamined at 15 (minimum) magnification factor.

- An accurate measurement of the defect size can be obtained by metallographic examination in accordance with 4.2.5.

          - The following fasteners shall be declared as nonconformant:

            - fasteners for failsafe applications if the size of any defect is larger than the size specified in ISO 6157-2 and ISO 6157-3;

            - fasteners for safelife applications if the size of any defect is larger than the size specified in clause 10.3 of ECSS-E-ST-30-01C.

Figure 4-1: Tolerance of headtoshank fillet profile

Table 4-1: Maximum allowed values of the extension C of the distorted area shown in Figure 4-1

| Nominal diameter, d (mm) | d < 5 | 5  d  7 | 8  d  10 | 11  d  16 | 17  d  24 | d > 24 |
| --- | --- | --- | --- | --- | --- | --- |
| C maximum (mm) | 1,00 | 1,5 | 2,5 | 3,5 | 4,5 | 5,0 |

### Metallurgical examination

          - Fasteners selected for metallurgical examination shall be cut and prepared for observation in accordance with state-of-the-art standard laboratory practice.

- Figure 4-2 shows the locations of microsections.

          - Fasteners when visually examined at a magnification of between 10 and 50 shall exhibit a continuous grain flow in the head area and headtoshank transition zone.

          - Z values shall be equal to or less than the maximum fillet radius R (Z  Rmax) as specified in the detail drawings of the customer specification document for threaded fasteners.

- Interruptions in grain flow within the area are defined by Z dimensions in Figure 4-3.

          - Fasteners when visually examined at a magnification of 50 shall exhibit continuous grain flow following the thread profile with maximum density of flow lines at thread roots.

- For details see Figure 4-4.

          - Fastener microstructure shall be visually inspected for internal defects at a magnification of 100 or higher in unetched condition.

          - Fastener microstructure shall be free from internal defects.

- Internal defects are voids, cracks, inclusions, gross alloy segregation and indication of overheating.

          - Surface coated or plated fasteners shall exhibit adequate thickness, uniformity and integrity of the protective layer.

          - For fasteners in Titanium alloy strength class 1100 MPa, DIN ISO 9152 shall apply.

(*) minimum required

Figure 4-2: Location of microsections for metallurgical examination

Z

Z

Z

Z

- Figure 4-3: Area delimiting interruptions in grain flow in the headtoshank region

- Figure 4-4: Example of a regular grain flow in a threaded surface

### Measurement of hydrogen content

          - Embrittlement by hydrogen absorption shall be prevented.

- Hydrogen contamination can cause embrittlement and degradation of mechanical properties of metals.

          - Hydrogen content in fasteners shall be measured by an approved vacuum fusion or vacuum extraction method.

- Samples of material can be extracted from the fastener head after the removal of any surface coating.

          - Hydrogen content in fully finished fasteners made of Titanium alloys shall not exceed 0,0125 %.

- Titanium alloys are particularly prone to embrittlement by hydrogen absorption.

### Outgassing and offgassing

          - Thermal vacuum outgassing test in accordance with ECSS-Q-ST-70-02C shall be carried out on fasteners with organic inserts or collars, lubricants or protective substances if exposed to vacuum during service.

          - Offgassing test in accordance with ECSS-Q-ST-70-29C shall be carried out on fasteners with organic inserts or collars, lubricants or protective substances if used in crew compartments of manned space vehicles.

## Mechanical testing

### General

          - With the exception of the cases covered in 4.3.6, 4.3.7 and 4.3.8, mechanical testing for quality control purposes shall be performed at room temperature (22  3) C and laboratory air, (55  10) % relative humidity.

          - Mechanical properties of fasteners shall be in accordance with the specifications in the customer specification document for threaded fasteners.

          - Mechanical testing shall be carried out in accordance with the sampling procedures and acceptance criteria specified in 4.4.2.3.

          - Fasteners shall be retained in an approved quarantine facility for record or traceability purposes or destroyed in accordance with company practice after mechanical testing.

- The test methods specified in this Standard are intended for quality control and acceptance only, ensuring that fastener properties are within the limit values specified in the customer specification document for threaded fasteners.

### Hardness test

#### General

          - Hardness tests shall be carried out in accordance with:

            - the Brinell Hardness Test (HB) in accordance with ISO 6506 (all parts); or

            - the Vickers Hardness Test (HV) in accordance with ISO 6507 (all parts); or

            - the Rockwell Hardness Test (HRC) in accordance with ISO 6508 (all parts).

          - Measured hardness values shall conform to the hardness values specified in the customer specification document for threaded fasteners.

#### Method

          - Hardness tests on fasteners shall be carried out on the circular surface at the end of the threaded portion of the fastener shank after removing any surface coating.

          - For fasteners with nominal diameter greater than 6 mm, hardness shall be measured in the centre of the circular surface and at two other locations at different distances from the centre of the surface, Figure 4-5.

          - For short fasteners which cannot be tensile tested (usually with a grip length less than twice the nominal diameter), the following steps shall be performed:

            - carry out Vickers hardness measurements on a longitudinal microsection of the shank;

            - measure hardness along the shank longitudinal axis.

          - When deemed necessary to check the heat treatment batch homogeneity by hardness testing, hardness tests shall be carried out after the completion of any heat treatment and before any rolling operation.

- Figure 4-5: Locations for hardness testing (indicated with cross symbol)

### Tensile test

#### Preconditions

          - The tensile test method in 4.3.3.2 shall apply to finished fasteners having:

            - a protruding head with grip length equal or greater than twice the nominal diameter, or

            - a countersunk head and an overall length equal or greater than three times the nominal diameter, or

            - a minimum length of 18 mm.

#### Method

          - Test jigs shall be designed and manufactured in accordance with ISO 3800.

          - Test jigs shall ensure a tensile loading parallel to the fastener main axis.

          - No torsional stress shall be induced by the assembly.

          - Specimens shall be assembled freely in the fixture without bending or forcing.

          - The bearing face of the threaded part of the jig, Figure 4-6 (a), or of the nut, Figure 4-6 (b), shall be located at least four pitches of distance from the unthreaded portion of the shank.

          - The nut threads shall be fully engaged.

          - A bolt length of at least two pitches shall protrude beyond the threaded part of the jig, Figure 4-6 (a), or the test nut, Figure 4-6 (b).

          - Test nuts shall be used only once.

          - When tested separately, axial load test of nuts shall be in accordance with clause 3.3 of ISO 9140.

          - Speed of testing shall be defined in terms of rate of separation of the two heads of the testing machine during a test.

          - Speed of testing shall not exceed 25 mm/min.

- Best practices is to maintain the speed of testing between 0,5 mm/min and 1,0 mm/min.

          - Static failure shall only be tolerated in the shank.

          - Fasteners with static failures occurring at the headtoshank fillets shall be identified as nonconformant.

          - The yield and ultimate tensile load of a tested fastener shall not be less than the values specified in the customer specification document for threaded fasteners.

          - The cross sectional area, S, used in the interpretation of the tensile test results, expressed in mm2, shall be assumed as the minimum of the two values S1 and S2 given by:

s1=π4d322−d2d32, or

s2=π4φmin2

where:

d2	is the nominal pitch diameter in mm;

d3	the thread root nominal diameter in mm; and

min	the diameter of the minimum fastener cross sectional area if not in the threaded portion.

### Shear test

#### Preconditions

          - The shear test method in 4.3.4.2 shall apply to:

            - finished fasteners of all sizes which meet one of the three requirements as specified in 4.3.3.1;

            - fasteners with stepped threads (shouldered fasteners).

#### Method

          - Shear test shall be carried out in doubleshear loading configuration.

- Figure 4-7 shows an example of doubleshear loading jigs.

          - The shear loads to failure shall be no less than the allowable values specified in the customer specification document for threaded fasteners.

### Fatigue test

#### General

          - Fatigue tests shall be carried out in accordance with ISO 3800.

#### Preconditions

          - The fatigue test method in 4.3.5.3 shall apply to finished fasteners of all sizes which meet one of the three requirements as specified in 4.3.3.1.

#### Method

          - Fasteners shall be loaded in tension in accordance with one of the loading schemes shown in Figure 4-5.

          - The fatigue test conditions shall be specified in the customer specification document for threaded fasteners in terms of:

            - type of load fluctuation (sinusoidal unless otherwise agreed);

            - stress range in MPa;

            - stress ratio (R);

            - frequency of load fluctuation in Hertz;

            - specified mean and minimum fatigue life in cycles.

          - The frequency of load fluctuation shall be

            - between 4 Hz and 250 Hz; and

            - such that the temperature of the test specimen measured at the first engaged thread is always less than 50C.

          - Stress calculation shall be based on the expressions for fastener cross sectional area given in 4.3.3.

          - Fatigue strength values shall be determined in the finite life range (failure of all test pieces before a predetermined number of stress cycles is reached) and in the transition range where, up to a predetermined number (typically 5  106 to 5  107) of stress cycles, failure as well as nonfailure occurs.

          - All the tested fasteners shall exceed the minimum number of cycles specified for each applied stress range in the customer specification document for threaded fasteners.

          - For fasteners with fatigue lives less than the expected mean fatigue life, failure shall not occur in the headtoshank fillet.

- No restrictions in failure location apply for fasteners with fatigue lives exceeding the expected mean fatigue life.

### Creep test

#### General

          - The creep tests shall be carried out in accordance with ISO 204.

          - Calculations shall be based on the expressions for fastener cross sectional area given in pppp.

- 1	Creep test is particularly recommended for Titanium alloy fasteners.

- 2	For details see Annex B.

#### Method

          - The percent elongation after fracture, the reduction of area at failure and the time to fracture shall be within the values specified in the customer specification document for threaded fasteners.

(l  four times the thread pitch and m  two times the thread pitch)

Figure 4-6: Loading schematic for tensile testing of threaded fasteners

- Figure 4-7: Schematic of an example of doubleshear loading jigs

### Corrosion test

#### General

          - Fasteners shall be tested for corrosion in accordance with ASTM B 117-07a.

#### Method

          - Sample geometry, exposure time and acceptance criteria shall conform to the requirements specified in the customer specification document for threaded fasteners.

          - Metallic fasteners shall not be in contact with carbon fibre composite materials.

- The reason is the considerable risk of corrosion.

### Stresscorrosion test

          - Stresscorrosion testing shall be carried out in accordance with ECSS-Q-ST-70-37C.

## Quality assurance

### General

          - The supplier (contractor or subcontractor) shall implement the quality assurance, inspection and quality control procedures specified herein before any supply activity.

          - The implementation of the procedures shall be maintained for the entire duration of the business agreement.

### Quality requirements

#### General

          - The supplier shall establish and implement adequate quality control actions and inspections to provide evidence of conformity to the product requirements.

- Quality control actions and inspections may be performed by the supplier or by different companies (e.g. manufacturers, test houses and external laboratories) entirely under the supplier’s direct responsibility.

          - The manufacturer shall have a quality assurance system in place (e.g. ISO 9001).

          - The supplier shall not use fasteners manufactured more than 10 years before use in space hardware.

- The reasons are possible timedependent degradation phenomena (e.g. corrosion, stress corrosion, design modifications, improvements in materials and manufacturing processes).

#### Quality control of materials

          - Selection and control of suitable materials for fastener fabrication shall be based on the requirements defined in ECSS-Q-ST-70-71C.

          - The supplier shall provide evidence that only materials in accordance with the customer specification document for threaded fasteners are used in the fabrication.

          - The supplier shall issue a raw material certificate (RMC) specifying: material standard designation, heat treatment, form, manufacturer, batch number, batch chemical analysis, batch tensile test results (0,2 % proof stress, ultimate stress and elongation) and batch hardness value.

          - In the case where NDI is requested in the customer specification document for threaded fasteners, the supplier shall include in the RMC the date of the NDI, name of inspector, NDI results with description of any nonconformance.

#### Sampling procedure

          - The supplier in agreement with the customer shall determine a sampling procedure in accordance with:

            - ISO 2859-1 for batchbybatch inspections; or

            - ISO 2859-2 for isolated batch inspections.

          - The supplier shall specify the selected sampling procedure in the customer specification document for threaded fasteners by defining a sampling plan.

          - The supplier shall define the batch acceptability criteria in terms of:

            - acceptance quality limit (AQL), if the batchbybatch inspection method is selected, or

            - limiting quality (LQ), if the isolated batch inspection is selected.

          - The supplier shall define sample size in terms of inspection levels.

- Table C-  gives the recommended inspection levels, LQ and AQL values to be used.

          - The supplier shall draw the specified sample units at random from the batch.

- A batch of fasteners is a set of fasteners of the same type and diameter, obtained from the same batch of raw material, manufactured by the same process and heat treated as one batch.

          - The supplier shall accept the batch only if the number of nonconforming units is less or equal to the acceptance level specified in the customer specification document for threaded fasteners.

          - The supplier shall reject any nonconforming units found during batch inspection.

#### Nonconforming batches

          - In the case where the number of nonconforming units is greater than the acceptance level specified in the customer specification document for threaded fasteners, the supplier shall reject the batch.

          - The supplier shall subject resubmission for inspection of rejected batches to the customer approval.

          - The customer shall determine the method of acceptance to be applied to resubmitted batches.

          - In resubmitted batches, the supplier shall re-examine or re-test all units in the batch.

          - The supplier shall remove all nonconforming units or replace them by conforming units.

          - On resubmission, the supplier shall indicate the nonconforming batches as resubmitted specifying the cause for previous nonconformance.

          - The supplier shall subject batches of fasteners for safelife applications to NDI in all their units.

#### Product conformance report

          - The supplier shall issue a product conformance report (PCR), in conformance with the DRD in Annex B, for each delivered batch of fasteners.

          - The supplier shall deliver the PCR to the customer together with the batch of fasteners.

#### Incoming inspection

          - On delivery the customer shall carry out an incoming inspection of the batch.

          - The customer shall establish if the information given in the PCR is complete, clear and satisfactory.

          - The customer shall verify that the fastener identification marks are consistent with the information given in the PCR.

          - For structural fasteners with nominal diameters larger than 4 mm (M4) which are not directly procured from a fastener manufacturer (i.e. procured through a distributor or vendor), the customer shall carry out: dimensional check, tensile test, chemical analysis, hardness test and nondestructive inspections in accordance with 4.2.4.

- A structural fastener is a fastener used in either the primary or secondary load path of a structure.

          - Sampling procedure shall be in accordance with 4.4.2.3.

          - Only qualified test laboratories shall carry out the tests.

          - The supplier shall provide evidence that the batch conforms to the customer specifications.

- (normative)
Customer specification document for threaded fasteners – DRD

  - DRD identification

    - Requirement identification and source document

This DRD is called from ECSS-Q-ST-70-46, requirement 1.1.1a.

    - Purpose and objective

Within the contractual relation between the customer and the supplier, the customer specification document for threaded fasteners specifies the technical and quality requirements, and the criteria and procedures to be used to assess the fulfilment of such requirements. The customer specification document for threaded fasteners is prepared by the customer, who sets the technical and quality requirements, in collaboration with the supplier, who agrees to the requirements and procedures.

This DRD does not define format, presentation or delivery requirements of the customer specification document for threaded fasteners.

  - Expected response

    - Scope and contents

          - Specifications

          - The document shall specify the following items:

            - The selected raw material in terms of: standard designation, heat treatment, form, minimum mechanical properties (hardness, 0,2 % proof stress, UTS, elongation and toughness).

            - The complete fastener manufacturing process in terms of all the single operations required from the raw material to obtain the finished product.

            - The nominal dimension, tolerance and geometry of the finished fastener.

            - Indication of fastener designation and thread type.

            - Technical drawings enclosed to the customer specification document for threaded fasteners.

            - Surface treatment of finished fasteners.

            - Minimum hardness values of finished fasteners.

            - Tensile mechanical properties of finished fasteners in terms of: load to yield, ultimate load and elongation to failure.

            - Minimum shear load to failure of finished fasteners.

            - Minimum and mean required fatigue strength of finished fasteners in terms of stress range versus fatigue cycles (S-N curves) at specified constant stress ratios.

            - Minimum creep properties of finished fasteners in terms of elongation, reduction of area and time to failure.

            - Corrosion requirements in terms of exposure time and acceptability criteria (maximum number and density of corrosion pits).

            - Stresscorrosion testing if requested.

            - Definition of mechanical test methods and conditions for e. f. g. h. i. j. and k. in accordance with the relevant clauses of this Standard and other applicable standards.

            - Quality control plan in terms of: identification marking, sampling procedure, sampling plan and nondestructive inspection (NDI) plan.

            - Definition of procedures and time schedule for handling, storage, transportation and delivery.

    - Special remarks

None.

- (normative)
Product conformance report (PCR) – DRD

  - DRD identification

    - Requirement identification and source document

This DRD is called from ECSS-Q-ST-70-46, requirement gggggg.

    - Purpose and objective

This DRD defines the contents of the PCR.

  - Expected response

    - Scope and contents

          - Contents

          - The PCR shall indicate:

            - batch supplier name/code;

            - date of batch manufacturing;

            - purchase order form;

            - raw or semifinished material supplier name/code;

            - date of raw or semifinished material production;

            - batch identification number and fastener identification marks;

            - reference to fastener specifications;

            - the raw material certificate (RMC) including a report of quality the inspections (destructive and nondestructive) carried out on the raw or semifinished material as specified in this document;

            - report of the fasteners quality control inspections (destructive and nondestructive) as specified in this document;

            - report of conformance/nonconformance and corrective actions;

            - any other relevant documentation.

    - Special remarks

None.

- (informative)
Inspection levels, acceptance quality limits (AQL) and limiting quality levels (LQ) for inspection of fasteners

Table C- : Inspection levels, acceptance quality limits (AQL) and limiting quality levels (LQ) for inspection of fasteners

| Inspection method | Highstrength steel | Stainless steel | Titanium alloys | Alloys for high temperature applications |
| --- | --- | --- | --- | --- |
| Hardness test | Inspection level S-3, AQL 0,65 LQ 5,0 % | Inspection level S-3, AQL 0,65 LQ 5,0 % | – | Inspection level II, AQL 0,65 LQ 2,0 % |
| Dimensional and surface control | Inspection level II, AQL 0,65 LQ 2,00 % | Inspection level II, AQL 0,65 LQ 2,00 % | Inspection level II, AQL 0,65 LQ 2,00 % | Inspection level II, AQL 0,65 LQ 2,0 % |
| Microstructural examination and chemical analysis | Inspection level S-1, AQL 1,5 LQ 12,5 % | Inspection level S-1, AQL 1,5 LQ 12,5 % | Inspection level S-1, AQL 1,5 LQ 12,5 % | Inspection level S-1, AQL 1,5 LQ 12,5 % |
| Inspection for surface defects by NDI | Inspection level II, AQL 0,065 LQ 0,5 % | Inspection level II, AQL 0,065 LQ 0,5 % | Inspection level II, AQL 0,065 LQ 0,5 % | Inspection level II, AQL 0,065 LQ 0,5 % |
| Inspection for surface defects by NDI – Safelife applications | 100 % batch inspection | 100 % batch inspection | 100 % batch inspection | 100 % batch inspection |
| Tensile test | Inspection level S-1, AQL 1,5 LQ 12,5 % | Inspection level S-1, AQL 1,5 LQ 12,5 % | Inspection level S-3, AQL 1,0 LQ 8,0 % | Inspection level S-1, AQL 1,5 LQ 12,5 % |
| Shear test | As specified by the customer (*) | As specified by the customer (*) | As specified by the customer (*) | As specified by the customer (*) |
| Corrosion test | As specified by the customer (*) | As specified by the customer (*) | As specified by the customer (*) | As specified by the customer (*) |
| Stresscorrosion test | As specified by the customer | As specified by the customer | As specified by the customer | As specified by the customer |
| Fatigue test | As specified by the customer (*) | As specified by the customer (*) | As specified by the customer (*) | As specified by the customer (*) |
| Creep test | As specified by the customer (*) | As specified by the customer (*) | As specified by the customer (*) | As specified by the customer (*) |
| Hydrogen content | As specified by the customer (*) | As specified by the customer (*) | Inspection level S-1, AQL 2,5 LQ 20,0 % | As specified by the customer (*) |
| Outgassing | As specified by the customer | As specified by the customer | As specified by the customer | As specified by the customer |
| Offgassing | As specified by the customer | As specified by the customer | As specified by the customer | As specified by the customer |
| (*) Test carried out on customer request. |  |  |  |  |

Bibliography

| ECSS-S-ST-00 | ECSS system – Description, implementation and general requirements |
| --- | --- |