Process Specification for Passivation and Pickling of Metallic Materials

Engineering Directorate Structural Engineering Division September 2006 National Aeronautics and Space Administration Lyndon B. Johnson Space Center Houston, Texas

Process Specification for Passivation and Pickling of Metallic Materials

| Prepared by: | Signature on file | 9/8/6 |
| --- | --- | --- |
|  | Jay Bennett Materials and Processes Branch/ES4 | Date |

| Approved by: | Signature on file | 9/8/6 |
| --- | --- | --- |
|  | Bradley S. Files, Chief Materials and Processes Branch/ES4 | Date |

| REVISIONS |  |  |
| --- | --- | --- |
| VERSION | CHANGES | DATE |
| Baseline | Original version | 5/96 |
| A | Formatting, modified callout, replacement of canceled QQ-P-35C with AMS-QQ-P-35, addition of pickling of Monel | 11/16/98 |
| B | Moved requirement from section 5 to section 6, allowed Type VI passivation for precipitation hardened stainless steels, added alternate embedded iron verification test, modified other periodic testing. | 5/17/01 |
| C | Allowed a shop option for choosing the passivation type in section 3.0; wording changes in section 6.2; wording changes in section 9.0, and added requirement that personnel certification be written; and modified the definition of “Passivation” in section 10. | 1/25/02 |
| D | Moved paragraph 3.1 to paragraph 6.1 and updated, renumbered and renamed remaining paragraphs in section 6. | 10/19/05 |
| E | Removed alternate embedded iron verification test. Reworded first paragraph of section 8. Added Custom 465 and 21-6-9 to list of alloys. | 09/08/06 |

1.0  	SCOPE

This process specification establishes technical requirements for the passivation of corrosion-resistant steel in the manufacture of JSC flight hardware.  In addition, it covers specialized pickling treatments for the removal of foreign particles from nickel-copper alloys.

Note:  All references in this document to passivation refer to corrosion-resistant steel and all references in this document to pickling refer to specialized pickling for the removal of foreign metal from the surface of nickel-copper alloys.

2.0  	APPLICABILITY

This process specification covers passivation treatments for use on austenitic, ferritic, martensitic, and precipitation-hardening corrosion-resistant steels.  In addition, it covers specialized pickling treatments for the removal of foreign particles from nickel-copper alloys.

3.0 	USAGE

This process specification shall be called out on the engineering drawing by using a drawing note that identifies the process specification and the type of passivation or pickling treatment to be used.  For example:

PASSIVATE PER NASA/JSC PRC-5002, TYPE VI.

If the specific passivation process is not critical to a particular design, the process type may be left off the drawing callout.   For example:

PASSIVATE PER NASA/JSC PRC-5002.

The decision to allow this shop option should be coordinated in advance with the responsible materials engineer.

The four types of passivation processes are as follows:

Type II		Medium-temperature nitric acid solution with sodium dichromate 			additive

Type VI		Low-temperature nitric acid solution

Type VII		Medium-temperature nitric acid solution

Type VIII		Medium-temperature, high-concentration nitric acid solution

Selection of the passivation type shall be made according to the following table:

| Type II | Type VI | Type VII | Type VIII |
| --- | --- | --- | --- |
|  | MP159 |  |  |
|  | MP35N |  |  |
|  | IN718 |  |  |
| ##### A286 | A286 |  | A286 |
| 13-8Mo | 13-8Mo* |  | 13-8Mo |
| 15-5PH | 15-5PH* |  | 15-5PH |
| 15-7Mo | 15-7Mo* |  | 15-7Mo |
| 17-4PH | 17-4PH* |  | 17-4PH |
| 17-7PH | 17-7PH* |  | 17-7PH |
| Custom 455 | ###### Custom 455* |  | Custom 455 |
| Custom 465 | ###### Custom 465* |  |  |
| 21-6-9 | 21-6-9 |  |  |
|  | AISI 201 | AISI 201 |  |
|  | AISI 202 | AISI 202 |  |
|  | AISI 301 | AISI 301 |  |
|  | AISI 302 | AISI 302 |  |
| AISI 303 |  |  | AISI 303 |
| AISI 303Se |  |  | AISI 303Se |
|  | AISI 304 | AISI 304 |  |
|  | AISI 304L | AISI 304L |  |
|  | AISI 304H |  | AISI 304H |
|  | XM-7 | XM-7 |  |
|  | AISI 304N | AISI 304N |  |
|  | AISI 305 | AISI 305 |  |
|  | AISI 308 | AISI 308 |  |
|  | AISI 309 | AISI 309 |  |
|  | AISI 309S | AISI 309S |  |
|  | AISI 309Cb | AISI 309Cb |  |
|  | AISI 310 | AISI 310 |  |
|  | AISI 310S | AISI 310S |  |
|  | AISI 311 | AISI 311 |  |
|  | AISI 314 | AISI 314 |  |
|  | AISI 315 | AISI 315 |  |
|  | AISI 316 | AISI 316 |  |
|  | AISI 316L | AISI 316L |  |
|  | AISI 316H |  | AISI 316H |
|  | AISI 321 | AISI 321 |  |
|  | AISI 321H |  | AISI 321H |
|  | AISI 329 | AISI 329 |  |
|  | AISI 347 | AISI 347 |  |
|  | AISI 347H |  | AISI 347H |
| AISI 347S |  |  | AISI 347S |
| AISI 347Se |  |  | AISI 347Se |
| AM350 |  |  | AM350 |
| AM355 |  |  | AM355 |
| Almar 362 |  |  | Almar 362 |
| AISI 403 |  |  | AISI 403 |
| AISI 405 |  |  | AISI 405 |
| AISI 409 |  |  | AISI 409 |
| AISI 410 |  |  | AISI 410 |
| AISI 414 |  |  | AISI 414 |
| AISI 416 |  |  | AISI 416 |
| AISI 416Se |  |  | AISI 416Se |
| AISI 420 |  |  | AISI 420 |
| AISI 429 |  | AISI 429 | AISI 429 |
|  |  | AISI 430 |  |
| AISI 430F |  |  |  |
| AISI 430FSe |  |  |  |
| AISI 431 |  |  | AISI 431 |
| AISI 434 |  | AISI 434 |  |
| AISI 436 |  | AISI 436 |  |
| AISI 440A |  |  | AISI 440A |
| AISI 440B |  |  | AISI 440B |
| AISI 440C |  |  | AISI 440C |
| AISI 440F |  |  | AISI 440F |
| AISI 440FSe |  |  | AISI 440FSe |
| AISI 442 |  | AISI 442 |  |
|  |  | AISI 446 |  |
| XM-27 |  | XM-27 |  |

Type VI is the preferred process when permitted by the table above.  It is the in-house process at JSC.  It utilizes no hazardous hexavalent chromium and is available in more metal finishing facilities. Older drawings should be changed so this process can be utilized whenever possible to save time and reduce costs.

Alloys not listed on the table above may be passivated to this specification, provided there is M&P approval for a specific passivation type on the engineering drawing or other process documentation.

Note that stainless steel parts that have hardened surfaces from nitriding, from carbonitriding, or from other similar diffusion treatments should not be passivated.  Severe corrosion and/or severe pitting of the hardened surfaces could readily occur.  In addition, stainless steels that are carburized should not be passivated, since the chromium combines with the carbon to form chromium carbides along the surface, which do not benefit from passivation.

Unless otherwise specified, the cleaning pre-treatment for passivation shall consist of an alkaline cleaning process according to the requirements of NASA/JSC PRC-5001.  However, no reference to PRC-5001 needs to be made on the drawing.

For pickling treatments of nickel-copper alloys, the standard engineering drawing callout shall be similar to the following example:

PICKLE PER NASA/JSC PRC-5002, TYPE L.

Type L refers to a solution of hydrochloric acid and ferric chloride (Formula L from p. 41 in Huntington Alloy IAI-21 (Second Edition, 1987).

4.0	REFERENCES

AMS-QQ-P-35	Passivation Treatments for Corrosion-Resistant Steel

ASTM B117		Standard Practice for Operating Salt Spray (Fog) Apparatus

Inco Publication 	Fabricating, Inco Alloys International, Inc., Second Edition,

IAI-21			1987.

QQ-P-35C			Federal Specification, Passivation Treatments for Corrosion-				Resistant Steel

MIL-STD-753C   	Corrosion-Resistant Steel Parts: Sampling, Inspection and 	Testing for Surface Passivation

- MATERIALS REQUIREMENTS

None

6.0  	PROCESS REQUIREMENTS

6.1	WORK INSTRUCTIONS

All work shall be performed to written procedures. The work instructions shall contain sufficient detail to ensure that the manufacturing process produces consistent, repeatable products that comply with this specification.

For work performed at JSC facilities, these work procedures consist of Detailed Process Instructions (DPI’s).

For contracted work, the contractor shall be responsible for preparing and maintaining, and certifying written work procedures that meet the requirements of this specification.

6.1     GENERAL REQUIREMENTS

All passivation of corrosion-resistant steel shall be conducted according to the requirements of AMS-QQ-P-35, with the modifications included in this process specification.   When no passivation type is specified, the metal finishing facility has the option of using any type process allowed for the alloy in the table above.

All pickling treatments shall be conducted within the guidelines of Huntington Alloy Booklet IAI-21 (Second Edition, 1987).

6.2	SPECIFIC REQUIREMENTS FOR PASSIVATION

The metal finishing facility shall maintain a record of the control procedures used for a given passivation treatment.  The passivation solution shall be analyzed weekly to verify that the concentration of nitric acid (and sodium dichromate if applicable) meet the specified ranges in AMS-QQ-P-35. The bath temperature of the passivation tank shall be verified before each use.

If a metal finishing facility uses the Type VI process for alloys in the table marked with an asterisk (*), the process bath shall be tested monthly to verify that the chloride concentration is less than 1000 ppm.  Testing of bath for chloride before parts are processed is also acceptable.  Shops that do not perform monthly chloride testing may not use the Type VI process for these alloys.

6.3	SPECIFIC REQUIREMENTS FOR PICKLING

For pickling operations, the acidic solution shall be controlled such that copper flash will not occur. General guidelines on the prevention and removal of copper flash are provided on p. 36 in Huntington Alloy IAI-21 (Second Edition, 1987).  The acidity levels shall be periodically monitored to ensure that the bath is at the proper initial strength.  Fresh solution should be made up when salts begin to crystallize on the sides of the tank.  Also, analysis of the pickling solution shall be done periodically to verify that the metallic content is below 150 grams per liter (g/L).  The solution must be discarded if the 150 g/L level is exceeded.

7.0	PROCESS QUALIFICATION

None required

- PROCESS VERIFICATION

The surface(s) being passivated or pickled shall be inspected for cleanliness prior to chemical treatment.

The post-treatment verification is detailed below in section 8.1 or 8.2.    The method used and result shall be included in the facility or vendor certificate of conformance of this process.

8.1	VERIFICATION OF PASSIVATION PROCESS

After the passivation process has been completed, the passivated components must exhibit chemically clean surfaces that show no etching, pitting, or frosting.  A slight discoloration will be allowed if the subject surface passes the water break free test.

Each lot of parts shall be tested to verify that embedded iron has been removed using one of the following 4 test methods that are detailed in AMS-QQ-P-35:

- Test Method 100 of MIL-STD-753C (water immersion test).

(2)	High humidity test per section 4.4.1.2 of AMS-QQ-P-35.

(3)	Salt spray testing for 2 hours according to the procedures of ASTM B117.

(4)	Test Method 102 of MIL-STD-753C (copper sulfate test).

8.2	VERIFICATION OF PICKLING PROCESS

Verification that the pickled surface is free of embedded iron or other metal shall be accomplished using one or more of the following test methods:

(1)	Scanning electron microscopy with backscatter mode detection and windowless energy dispersive spectroscopy can be utilized.  This is a very expensive technique and should be limited to small items of a limited quantity.

- Test Method 103 of MIL-STD-753C (Potassium Ferricyanide-Nitric Acid Solution) is an ultra-sensitive technique for small batches that can be used if inspectors have proper training in its use.

(3)	A salt spray test utilizing a solution of 1% sodium chloride for 12-24 hours can be used for large scale testing.  Any free iron on the surface will appear as rust spots.

9.0	TRAINING AND CERTIFICATION OF PERSONNEL

Personnel performing passivation and pickling treatments of metallic materials shall be certified to conduct this process by their supervisor.  This certification shall be written.  If these processes are to be performed by an outside vendor, the development of an appropriate training program shall be the responsibility of the vendor.

10.0	DEFINITIONS

Passivation		The chemical treatment of a stainless steel alloy or iron based superalloy with a mild oxidizer, such as nitric acid, to remove free iron or other contaminants embedded in the surface, for example tool steel from machining.  Passivation treatment also produces an oxide film with superior corrosion resistance to the oxide film that occurs naturally.  Passivation is not generally effective in removing oxide scale or heat tint.

Pickling			The chemical treatment of metallic materials with an aqueous acid solution that results in the removal of surface oxides or scale formed during heating.  This method also removes other foreign metals and other substances.

Water Break		A test to determine if a surface is chemically clean by

Free Test			the use of a distilled water rinse.  If the surface is clean, the water will break and spread across the surface in a sheet-like manner.  A contaminated sur-face will cause the water to form droplets and “bead”.

Corrosion-resistant 	An alloyed steel that contains chromium in excess of

Steel			10.5 wt-%.