Process Specification for Magnetic Particle Inspection

Engineering Directorate Structural Engineering Division February 2007 National Aeronautics and Space Administration Lyndon B. Johnson Space Center Houston, Texas

Process Specification for Magnetic Particle Inspection

| Prepared by: | ### Signature on File |  | 02/14/07 |
| --- | --- | --- | --- |
|  | Ajay Koshti, ES4 |  | Date |

| Approved by: | ### Signature on File |  | 02/XX/07 |
| --- | --- | --- | --- |
|  | Bradley S. Files, Chief, Materials and Processes Branch/ES4 |  | Date |

| REVISIONS |  |  |
| --- | --- | --- |
| VERSION | CHANGES | DATE |
| Baseline | Original version | 7/22/99 |
| A | Reviewed document per QMS requirements. Updated division name, organization codes, and document numbers. | 12/19/02 |
| B | Deleted SNT-TC-1A and MSFC-STD-1249. Added NASA-STD-5009 and NASA-STD-5019. | 02/14/07 |

1.0	SCOPE

This process specification establishes the minimum requirements for magnetic particle inspection of ferromagnetic materials and components.

# 2.0	APPLICABILITY

This specification is applicable to in-process, final, and in-service magnetic particle inspections to detect discontinuities that are on or near the surface of ferromagnetic materials.  Magnetic particle inspection is not applicable to nonferromagnetic metals and alloys.

3.0	USAGE

This specification shall be invoked by including an inspection note on the applicable engineering drawing or by reference in a Process Specification, Task Performance Sheet, Discrepancy Report/Material Review Record, or other appropriate document.  The engineering drawing or referencing document shall specify the criteria by which components are judged acceptable. Where acceptance criteria are not otherwise specified the criteria in Section 3.3 shall apply.  Other acceptance criteria, such as those in MIL-STD-1907, may be used as appropriate.  When there are different acceptance criteria for different areas on a component, the drawing shall be zoned with the acceptance criteria identified for each zone.  If the number of components to be inspected and the amount of coverage of each component is not specified, all components shall be examined and shall receive 100 percent magnetic particle coverage.

The standard magnetic particle inspection note for flight hardware and critical ground equipment is given in Figure 1.

Figure 1.

PERFORM WET FLUORESCENT MAGNETIC PARTICLE INSPECTION PER JSC PRC-6505.

An example of a magnetic particle inspection note for non-critical ground equipment using the acceptance criteria in MIL-STD-1907 is given in Figure 2.

Figure 2.

PERFORM MAGNETIC PARTICLE INSPECTION PER JSC PRC-6505.  ACCEPTANCE CRITERIA PER MIL-STD-1907, GRADE A.

3.1	INSPECTION SEQUENCE

The stage in the manufacturing process where magnetic particle inspection is performed should be specified on the engineering drawing or in the referencing document.  Final magnetic particle inspection shall be performed after completion of all manufacturing operations that can generate surface or near surface discontinuities.  These operations include, but are not limited to, forging, heat treating, plating, passivation, cold forming, welding, grinding, straightening, machining, and proof loading.  In general, components should be inspected prior to the application of any coatings.  Components heat treated to an ultimate tensile strength of 180 ksi or higher that are subsequently electroplated shall be inspected after the electroplating operation.

3.2	SPECIAL NDE OF FRACTURE CRITICAL COMPONENTS

When implementation of fracture control requirements necessitates Special Nondestructive Evaluation (NDE) of a fracture critical component, the requirement for Special NDE shall appear in the inspection note as shown in Figure 3.   When Special NDE is required, the specific inspection procedure and inspector shall be qualified in accordance with Section 7.0.

Figure 3.

PERFORM WET FLUORESCENT MAGNETIC PARTICLE INSPECTION PER JSC PRC-6505.  SPECIAL NDE QUALIFICATION REQUIRED.

3.3	ACCEPTANCE CRITERIA

The engineering drawing or referencing document shall indicate the criteria by which components are judged acceptable.  Where acceptance criteria are not otherwise specified the following criteria shall apply:

a.	Linear indications – all linear indications, regardless of length, shall be cause for rejection of the component.

b.	Single rounded indications – a single rounded indication greater than 0.030 inches in diameter shall be cause for rejection of the component.

c.	Multiple rounded indications - two or more rounded indications each less than 0.030 inches in diameter but separated by less than 0.030 inches shall be cause for rejection of the component.

4.0	REFERENCES

The following specifications, standards, and handbooks form a part of this document to the extent specified herein.  All documents listed are assumed to be the current revision unless a specific revision is listed.  In the case of conflict between this specification and the technical requirements cited in other referenced documents, the requirements of this document take precedence.

ASTM E 1444		Standard Practice for Magnetic Particle Inspection

MIL-STD-1907	Inspection, Liquid Penetrant and Magnetic Particle, Soundness Requirements for Materials, Parts, and Weldments

NASA-STD-5009	Nondestructive Evaluation Requirements for Fracture Critical Metallic Components

NAS 410				NAS Certification & Qualification of Nondestructive

Test Personnel

# NASA-STD-5019	fracture Control Requirements for Spaceflight Hardware

NASA-STD-5003	Fracture Control Requirements for Payloads Using the Space Shuttle

SSP 30558	Fracture Control Requirements for Space Station

The following references were used to develop this process specification:

SOP-007.1	Preparation and Revision of Process Specifications (PRC’s)

JSC 8500	Engineering Drawing System Requirements

5.0	MATERIAL REQUIREMENTS

Inspection materials shall meet the requirements in ASTM E 1444.

6.0	PROCESS REQUIREMENTS

6.1	GENERAL

Magnetic particle inspections shall be performed in accordance with ASTM E 1444 except as modified by this specification. Unless otherwise specified, the wet fluorescent particle continuous method shall be used for flight hardware and critical ground equipment.

6.2	WRITTEN PROCEDURES

A detailed written procedure shall be prepared for each part to be inspected.  The procedure shall meet the requirements of this specification and shall ensure the consistency and reproducibility of the inspection at the required sensitivity level.  General procedures covering a variety different parts may be used provided they meet the requirements of this specification and clearly apply to the parts to be inspected.  When general procedures are used, a written part specific technique shall be prepared.  At a minimum, the part specific procedure or the general procedure and part specific technique shall cover all of the information required by ASTM E 1444.

For work performed at JSC facilities, written procedures should consist of Detailed Process Instructions (DPIs) selected for use from the DPI-6505-XX series of work instructions.

6.3	FRACTURE CRITICAL COMPONENTS

Magnetic particle inspection of fracture critical components shall be performed in accordance with the process requirements in NASA-STD-5009.  The requirements in NASA-STD-5009 not otherwise covered in this specification are included in the following:

a.	Examination surfaces must be easily accessible with a surface roughness of 125 RMS or better.

b.	Inspections shall be performed prior to the application of any coatings.

c.	The wet fluorescent particle continuous method shall be used.

d.	Local magnetic field strength shall be verified using an artificial flaw shim or a Hall effect probe.  When a Hall effect probe is used, readings shall be correlated with an artificial flaw shim in an equivalent part location.  Pie gages are not acceptable for verifying field strength.

When Special NDE is specified by the engineering drawing or referencing document, the inspection procedure and inspector shall be qualified in accordance with Section 7.0.

7.0	SPECIAL NDE QUALIFICATION

Use of Special NDE in accordance with NASA-STD-5019, NASA-STD-5003 or SSP 30558 requires formal demonstration of the capability to detect flaws at least as small as the critical initial crack size for the specific component to a 90/95 detection level. Each procedure, procedure application, and operator must demonstrate the required capability.  Requests for Special NDE qualification shall be directed to the JSC Materials and Processes Branch (ES4).

## 8.0	DEVIATIONS AND WAIVERS

Any deviations or waivers regarding the use of this process specification shall be requested in writing.  This request shall be directed to the JSC Materials and Processes Branch (ES4) with the appropriate justification and rationale.  A written response will be provided upon such a request.

9.0	TRAINING AND CERTIFICATION OF PERSONNEL

Personnel performing magnetic particle inspections shall be qualified and certified in accordance with NAS 410. Personnel making accept/reject decisions shall be certified to at least Level II. Personnel performing inspections on fracture critical components shall, at a minimum, be certified to Level II.

For work performed at JSC facilities, these requirements may be satisfied by the training and certification of personnel per the TI-6505-XX series of Training Instructions (TIs).

10.0	DEFINITIONS

90/95  	The point where the 95% lower confidence bound on the

Probability of Detection (POD) vs. flaw size curve crosses 90% POD or 90% POD with 95% lower confidence bound.

Discontinuity	An intentional or unintentional interruption in the physical structure or configuration of a material or component that may be detectable by nondestructive testing; a flaw. Discontinuities are not necessarily rejectable.

Final Inspection	The final inspection performed for the acceptance of the component.

Fracture Critical	Classification which assumes that fracture or failure of the

Component	component resulting from the occurrence of a crack will result in a catastrophic hazard.  Fracture critical components will be identified as such on the engineering drawing.

Indication	Evidence of a discontinuity that requires interpretation to determine its significance.

In-Process	Inspections which occur during manufacturing before a component is in final form.

In-Service	Inspections performed on components that are in use or storage.

Linear Indication	Penetrant indication with a length to width ratio of 3:1 or greater.

Rounded	Penetrant indication with a length to width ratio of less than

Indication	3:1.

Special NDE	A fracture control term denoting nondestructive inspection personnel, procedures, and equipment with a demonstrated capability to reliably (90/95) detect flaws smaller than those normally detected by typical procedures.