Process Specification for the Installation of Key-retained Screw Thread Inserts

Engineering Directorate Structural Engineering Division February 2007 National Aeronautics and Space Administration Lyndon B. Johnson Space Center Houston, Texas

Process Specification for the Installation of Key-retained Screw Thread Inserts

| Prepared by: |  |  |  |
| --- | --- | --- | --- |
|  | Jay E. Bennett Materials and Processes Branch ES4 |  | Date |
| Approved by: | Bradley S. Files, Chief Materials and Processes Branch ES4 |  | Date |

| REVISIONS |
| --- |
| VERSION | CHANGES | DATE |
| -- | Original version | 5/31/96 |
| A | Included reference to sealing specification, improved the verification section, and reordered the sections. | 7/29/99 |
| B | Added three new paragraphs to section 3. In the tables in appendix A, created a separate column for NAS part numbers, corrected two typos in part number designations, and rounded off tap drill depths to nearest .005”. | 10/18/99 |
| C | Changed Division name. Revised Section 6.1 (Work Instructions), and revised Section 9.0 (Training). | 10/2004 |
| D | Updated document numbers and names in Section 4.0 (References) | 2/2007 |

1.0  	SCOPE

This process specification establishes requirements for the installation of key-retained inserts and studs.

2.0  	APPLICABILITY

This specification shall be applicable whenever the installation of key-retained inserts and studs is invoked per section 3.0, “Usage”.

3.0  	USAGE

This process specification shall be called out on the engineering drawing by using a drawing note.  For example:

INSTALL KEY-RETAINED INSERTS PER NASA/JSC PRC-9006.

Most hole preparation details do not need to be specified on the engineering drawing because the requirements are covered in this PRC.  Through-holes are preferred, but must be specified on the engineering drawing.  Use of a plug tap is standard for blind holes.  When use of a bottom tap is necessary, it shall be specified on the engineering drawing as follows:

USE BOTTOM TAP.

The depth of the drill hole for plug taps is the sum of the maximum insert length, the maximum insert depth below the surface, and the length of five incomplete threads.  The depth of the drill hole for bottom taps is the sum of the maximum insert length, the maximum insert depth below the surface, and the length of three incomplete threads.  Standard drill hole depths are found in Tables 1, 2, 3, and 4 (see Appendix A).  Alternate drill hole depths may be used, as long as minimum full thread depth is maintained, but the alternate drill hole depth must be specified on the engineering drawing.

The depth of the drilled hole does not include the material removed by point of the drill.  The standard drill point has an included angle of 60(.  A 135( or flat bottom drill bit can be utilized if necessary, but must be called out on the engineering drawing.

The hole preparation for self-locking and non-self-locking inserts is identical except for the larger sizes.  Separate hole preparation dimensions are given for these sizes.

This specification may be used to install non-standard key-retained screw thread inserts.   The hole preparation dimensions for these inserts shall be called out on the engineering drawing.

Wet installation of inserts with corrosion preventative primer is standard for aluminum and for dissimilar metal joints.  Use the following callout:

SEAL INSERT PER NASA/JSC PRC-4004.

In some design cases, sealant may not be necessary, but the decision not to use sealant should be reviewed in advance with Materials and Processes Branch (ES4) personnel.

4.0  	REFERENCES

The following references were used to develop this process specification:

SOP-007.1	Preparation and Revision of Process Specifications

JPR 8500.4	Engineering Drawing System Manual

The following documents are called out as an extension of the requirements given in this specification:

FED-STD-H28/2B	Screw-Thread Standards for Federal Services, Section 2, Unified Inch Threads -- UN And UNR Thread Forms

MSFC-SPEC-250	Protective Finishes for Space Vehicle Structures and Associated Flight Equipment, General Specification for

MS51830			Insert, Screw-Thread, Locked In, Key-Locked, Miniature and Lightweight

MS51831			Insert, Screw-Thread, Locked In, Key-Locked, Heavy Duty

MS51832			Insert, Screw-Thread, Locked In, Key-Locked, Extra Heavy Duty

MS51833			Stud, Locked In, Key-Locked, Regular Duty

MS51834			Stud, Locked In, Key-Locked, Heavy Duty

MS51835			Inserts and Studs, Locked in, Key Locked, Hole Dimensions for and Assembly of

NAS1394			Insert-Threaded Metal, Lightweight, Self-Locking, and Non Self-Locking

NAS1395 			Insert-Threaded Metal, Heavy Duty, Self-Locking, and Non Self-Locking

5.0	MATERIAL REQUIREMENTS

None identified.

6.0	PROCESS REQUIREMENTS

6.1  	WORK INSTRUCTIONS

All work shall be performed to written procedures. The work instructions shall contain sufficient detail to ensure that the manufacturing process produces consistent, repeatable products that comply with this specification.

For work performed at JSC facilities, these work procedures consist of Detailed Process Instructions (DPI’s).

For contracted work, the contractor shall be responsible for preparing and maintaining, and certifying written work procedures that meet the requirements of this specification.

6.2	HOLE PREPARATION AND DRILLING

Hole preparation shall be in accordance with Tables 1,2, 3, and 4 in Appendix A.  In addition, tapped holes shall be drilled to the diameter and depth specified in the Appendix A tables.

6.3	COUNTERSINK

The edge of the recess shall be countersunk.  The angle of countersink shall be 100 degrees inclusive.

6.4	TAPPING

Threads in the parent material shall meet FED-STD-H28/2B, UN thread form, with a modified minor diameter, tolerance class 2B, except when noted as NS. Minimum full thread depth requirements shall be as noted in the Appendix A tables.

6.5   HOLE FINISH

The hole protective finish shall be completed as-specified on the engineering drawing.

6.6	FLUSHNESS

Miniature inserts shall be 0.005 to 0.015 in. below the surface of the parent material after installation.   Lightweight, heavy-duty, and extra heavy-duty inserts shall be 0.010 to 0.030 inch below the surface of the parent material after installation.  The driven keys shall be flush or below the surface of the parent material.

6.7	BROACHING

When key inserts are installed into materials where the minimum ultimate tensile strength is greater than 80,000 pounds per square inch, the slots for the locking keys shall be broached.  The slots shall also be broached for aluminum alloys that are defined as non-corrosion resistant by MSFC-SPEC-250.

7.0	PROCESS QUALIFICATION

The key insert installation process shall be qualified and accepted prior to assembly of production parts.  This qualification shall provide documented evidence that the installation procedures are capable of meeting the requirements of this process specification and the engineering drawing.  Any change to the procedure or insert type shall require re-qualification.

8.0	PROCESS VERIFICATION

The requirements in sections 6.2	(Hole Preparation and Drilling), 6.3 (Counter-sink), 6.4 (Tapping), and 6.6 (Flushness) shall be verified by inspection.

9.0  	TRAINING AND CERTIFICATION OF PERSONNEL

This process shall be performed by personnel qualified through training or experience and certified by their supervision to conduct the process.

10.0	DEFINITIONS

None.

APPENDIX A – INSERT INSTALLATION DATA

Table 1-- Miniature Insert Installation Data

| Insert | Hole Preparation |
| --- | --- |
| Part Number | Internal Thread (Modified Minor Diameter) | Tap Drill Diameter | Plug Tap Drill Depth (0.010 | Bottom Tap Drill Depth ( 0.010 | CSK Dia +0.010 -0.000 | Minimum Full Thread Depth |
| MS51830XX101 | 0.164-32 | .137 .133 | .305 | .245 | .166 | .140 |
| MS51830XX102 | 0.190-32 | .164 .160 | .355 | .295 | .194 | .160 |
| MS51830XX103 | 0.216-28 | .191 .186 | .380 | .305 | .220 | .160 |
| MS51830XX104 | 0.250-28 | .231 .227 | .430 | .355 | .255 | .210 |

Table 2-- Lightweight Insert Installation Data

| Insert Part Number | Hole Preparation |
| --- | --- |
| NAS Series | MS Series | Internal Thread (Modified Minor Diameter) | Tap Drill Diameter | Plug Tap Drill Depth (0.010 | Bottom Tap Drill Depth ( 0.010 | CSK Dia +0.010 -0.000 | Minimum Full Thread Depth |
| NAS1394XX3 | MS51830XX105 MS51830XX201 MS51833XX101 MS51833XX201 | 0.3125-18 | .276 .271 | .635 | .525 | .323 | .370 |
| NAS1394XX4 | MS51830XX106 MS51830XX202 MS51833XX102 MS51833XX202 | 0.3750-16 | .336 .331 | .735 | .610 | .385 | .430 |
| NAS1394XX5 | MS51830XX107 MS51830XX203 MS51833XX103 MS51833XX203 | 0.4375-14 | .401 .396 | .840 | .695 | .447 | .500 |
| NAS1394XX6 | MS51830XX108 MS51830XX204 MS51833XX104 MS51833XX204 | 0.5000-13 | .457 .452 | .930 | .775 | .510 | .560 |
| NAS1394XX7 | MS51830XX109 MS51830XX205 MS51833XX105 MS51833XX205 | 0.5625-12 | .521 .515 | 1.025 | .855 | .572 | .620 |
| NAS1394XX8 | MS51830XX110 MS51830XX206 MS51833XX106 MS51833XX206 | 0.6250-11 | .583 .577 | 1.125 | .945 | .635 | .680 |

Table 3 -- Heavy Duty Insert Installation Data

| Insert Part Number | Hole Preparation |
| --- | --- |
| NAS Series | MS Series | Internal Thread (Modified Minor Diameter) | Tap Drill Diameter | Plug Tap Drill Depth (0.010 | Bottom Tap Drill Depth ( 0.010 | CSK Dia. +0.010 -0.000 | Minimum Full Thread Depth |
| NAS1395XX08 | MS51834XX101 MS51834XX201 | 0.3125-18 | .276 .271 | .635 | .525 | .323 | .370 |
| NAS1395XX3 | MS51831XX101 MS51831XX201 MS51834XX102 MS51834XX202 | 0.3750-16 | .336 .331 | .670 | .545 | .385 | .370 |
| NAS1395XX4 | MS51831XX102 MS51831XX202 MS51834XX103 MS51834XX203 | 0.4375-14 | .401 .396 | .775 | .635 | .447 | .430 |
| NAS1395XX5 | MS51831XX103 MS51831XX203 MS51834XX104 MS51834XX204 | 0.5000-13 | .457 .452 | .865 | .715 | .510 | .500 |
| NAS1395XX6 | MS51831XX104 MS51831XX204 MS51834XX105 MS51834XX205 | 0.5625-12 | .521 .515 | .960 | .795 | .572 | .560 |
| NAS1395XX7 | MS51831XX105 MS51831XX205 MS51834XX106 MS51834XX206 | 0.6250-11 | .583 .577 | 1.125 | .945 | .635 | .680 |
| NAS1395XX8 | MS51831XX106 MS51831XX206 MS51834XX107 MS51834XX207 | 0.6875-11NS | .646 .640 | 1.185 | 1.005 | .700 | .750 |
| NAS1395XX9 | MS51831XX107 MS51831XX207 MS51834XX108 MS51834XX208 | 0.8125-16 | .771 .765 | 1.170 | 1.045 | .822 | .940 |
| NAS1395XX10 | MS51831XX108 MS51831XX208 MS51834XX109 MS51834XX209 | 0.875-14 | .833 .827 | 1.275 | 1.135 | .885 | 1.000 |
|  | MS51831XX109 MS51831XX209 MS51834XX110 MS51834XX201 | 1.125-12 | 1.067 1.061 | 1.585 | 1.420 | 1.145 | 1.310 |
|  | MS51831XX109L MS51831XX209L MS51834XX110L MS51834XX201L | 1.125-12 | 1.067 1.061 | 1.710 | 1.545 | 1.145 | 1.440 |
|  | MS51831XX110 MS51831XX210 MS51834XX111 MS51834XX211 | 1.25-12 | 1.192 1.186 | 1.710 | 1.545 | 1.270 | 1.440 |
|  | MS51831XX110L MS51831XX210L MS51834XX111L MS51834XX211L | 1.25-12 | 1.192 1.186 | 1.835 | 1.670 | 1.270 | 1.560 |
|  | MS51831XX111 MS51831XX211 MS51834XX112 MS51834XX212 | 1.375-12 | 1.317 1.311 | 1.835 | 1.670 | 1.395 | 1.560 |
|  | MS51831XX111L MS51831XX211L MS51834XX112L MS51834XX212L | 1.375-12 | 1.317 1.311 | 1.960 | 1.795 | 1.395 | 1.680 |

Table 4 -- Extra Heavy Duty Insert Installation Data

| Insert | Hole preparation |
| --- | --- |
| Part Number | Internal Thread (Modified Minor Diameter) | Tap Drill Diameter | Plug Tap Drill Depth (0.010 | Bottom Tap Drill Depth ( 0.010 | CSK Dia. +0.010 -0.000 | Minimum Full Thread Depth |
| MS51832XX101 MS51832XX201 | .4375-14 | .401 .396 | .715 | .570 | .447 | .370 |
| MS51832XX102 MS51832XX202 | .500-13 | .457 .452 | .805 | .650 | .510 | .440 |
| MS51832XX103 MS51832XX203 | .5625-12 | .521 .515 | .900 | .730 | .572 | .500 |
| MS51832XX104 MS51832XX204 | .625-11 | .583 .577 | 1.000 | .820 | .635 | .560 |
| MS51832XX105 MS51832XX205 | .6875-11NS | .646 .640 | 1.125 | .945 | .700 | .680 |
| MS51832XX106 MS51832XX206 | .8125-16 | .771 .765 | 1.045 | .920 | .822 | .750 |
| MS51832XX107 MS51832XX207 | .875-14 | .833 .827 | 1.215 | 1.070 | .885 | .940 |
| MS51832XX108 MS51832XX208 | 1.000-12 | .942 .936 | 1.335 | 1.170 | 1.020 | 1.000 |
| MS51832XX109 MS51832XX209 | 1.250-12 | 1.192 1.186 | 1.587 | 1.420 | 1.270 | 1.310 |
| MS51832XX109L MS51832XX209L | 1.250-12 | 1.192 1.186 | 1.712 | 1.545 | 1.270 | 1.440 |
| MS51832XX110 MS51832XX210 | 1.375-12 | 1.317 1.311 | 1.712 | 1.545 | 1.395 | 1.440 |
| MS51832XX110L MS51832XX210L | 1.375-12 | 1.317 1.311 | 1.837 | 1.670 | 1.395 | 1.560 |
| MS51832XX111 MS51832XX211 | 1.500-12 | 1.442 1.437 | 1.837 | 1.670 | 1.520 | 1.560 |
| MS51832XX111L MS51832XX211L | 1.500-12 | 1.442 1.437 | 1.962 | 1.795 | 1.520 | 1.680 |